## Slide 1
S. Viarengo1,2, P. Ferracin2, Laura Savoldi1, Fabio Freschi1, X. Wang2, L. Brouwer2
1Politecnico di Torino, Torino, Italy
2Lawrence Berkeley National Lab, Berkeley, CA
MDP Collaboration Meeting, Virtual, 20/09/2022
Multiphysics modeling for REBCO CORC® cables based on T-A formulation

## Slide 2: Outline
Framework and aim of the work
Tape modeling
  REBCO design
  Critical current density evaluation
  Mathematical model
  Model setup, geometry and mesh, results
  Thermal recovery test
CORC® modeling
  VPI test in LBL
  Cable design and parameters
  CORC® thermal model
  Model setup and new boundary conditions
  2 tapes: thermal disturbance test
  6 tapes CORC® results
Conclusion and next steps
References

## Slide 3: Framework and aim of the work
[Status of CORC® cables and wires for use in highfield magnets and power systems a decade after their introduction, D.C. Van der Laan et al, 2019]
C2 wire layout
(Courtesy of LBL)
Jc characterization of a homogenous material for the single tape
Validation on a straigth Conductor on Round Core Cable (CORC®)
REBCO CORC® cable for CCT application
Multiscale approach

## Slide 4: Tape modeling

## Slide 5: REBCO Tape design
Thermal-physical properties as function of temperature θ and RRR
λ, ρ weigthed on the cross section and cp on the mass
Copper stabilizer
20 μm
REBCO
1.6 μm
Buffer zone
0.4 μm
Substrate
50 μm
Silver layer
1.6 μm
2.2 mm
95.2 μm
Rcu
Rsilver
Rsubstrate
RYBCO
Rcu
Rsilver
i
icu
icu
isilver
iYBCO
isub
isilver
Power Law
SCS-4050 by SuperPower 2008
[Two-Dimensional Anisotropic Model of YBCO Coated Conductors, Casali et. al, 2015]
[In-Field Electrical Resistance at 4.2 K of REBCO Splices, J. Fleiter and A. Ballarino, et. al, 2017]
y
density

## Slide 6: Critical current density
Parameter | Value | Unit
Parameter | Value | Unit
[Performance correlation between YBa2Cu3O7-δ coils and short samples for coil technology development, X. Wang et. al, 2016]
[Self-Consistent Modeling of the Ic of HTS Devices: How Accurate do Models Really Need to Be?, Grilli et. al, 2014]
* Blue: 4.2 K, Red: 77 K

## Slide 7: Mathematical model (1)
Governing equations:
  T-formulation (Tape)
  A-formulation
  (Whole domain)
Thin shell approximation:
Sum of two contributions:
Joule losses from T-formulation
Cooling from liquid nitrogen bath
REBCO tape
Air domain
  Heat conduction equation (Tape)
[Study of magnetization loss of CORC cables using 3D T-A formulation, Y. Wang, 2019]
[3D quench modeling base on T-A formulation for high temperature superconductor CORC cables, Y. Wang, 2019]

## Slide 8: Mathematical model (2)
y
x
z
T
Jz
Jy=0
Jx=0
Jz
T
Final governing equation:
n

## Slide 9: Tape thermal model
Thermal model
Free convection
y
x
z

## Slide 10: Model set up and boundary conditions
Injection of a ramp of current on the tape cross section
Tape immersed in a bath of liquid nitrogen @ 77 K
External field applied
2D/3D simulations
REBCO tape
Air domain

## Slide 11: Geometry and mesh
Air domain: tetrahedral mesh
Tape domain: triangular mesh
Elements in tape width: 50
Dofs: ~ 13,000

## Slide 12: Results: V-I curve in self-field at @ 77 K
Good agreement on V-I characteristic
Magnetic flux induced
(T)

## Slide 13: Results: V-I curves with vertical field applied at @ 77 K
Strong Ic degradation
N-value: 25
REBCO
[Isotropic round-wire multifilament cuprate superconductor for generation of magnetic fields above 30 T, Larbalestier D.C., et. al, 2014]

## Slide 14: Results: thermal
Temperature map evolution
Trend in agreement with
V-I curve
(K)
dTmax = 80 mK
!
Ic
(A)

## Slide 15: Model a recovery!
5 mm
0.5 mm
External heat source imposed on the center of the tape

## Slide 16: Recovery Results

## Slide 17: CORC® modeling

## Slide 18: VPI test in LBNL
[Developing a Vacuum Pressure Impregnation Procedure for CORC® Wires, J. Sterne et. al, MT27, 2021]
[Distributed fiber optic sensing to identify locations of resistive transitions in REBCO conductors and magnets, L. Luo et. al, MT27 2021]
3 layers
2 REBCO tapes/layer (6 tapes total)
2.8 mm diameter
3 set of experiments:
  Set 1: straigth CORC® cable, before bending
  Set 2: bended CORC® cable, before epoxy impregnation
  Set 3: bended CORC® cable, after epoxy impregnation

## Slide 19: Cable layout
Din
pitch
Copper stabilizer
5 μm
REBCO
1.6 μm
Buffer zone
0.4 μm
Substrate
20 μm
Silver layer
1.6 μm
2.02 mm
45.2 μm
Parameter | Value | Unit
Parameter | Value | Unit

## Slide 20: Strain dependance: critical current density
20
[Status of CORC® cables and wires for use in highfield magnets and power systems a decade after their introduction, Van der Laan D.C. et al, 2019]
Maximum strain:

## Slide 21: CORC® thermal model
Thermal model
y
x
z

## Slide 22: Boundary condition!
Minimum domain: a CORC® pitch
Total current imposed in the last boundary
Current sharing between tapes
Periodic boundary conditions (PBC)
New BC!

## Slide 23: Thermal disturbance
External heat source imposed on the center of the tape

## Slide 24: Thermal disturbance: results

## Slide 25: Geometry and mesh
Air: tetrahedral mesh
Tapes: Triangular mesh
Dofs ~ 91,000

## Slide 26: 6 tapes CORC® @ 200 A (1)
(T)
Magnetic flux induced
Non-homogeneous current distribution: higher current flowing in the inner layer
!
Current density distribution
(A/m2)

## Slide 27: 6 tapes @ 200 A (2)
T distribution
(A/m)

## Slide 28: Conclusions and next steps
Multiphysics (thermal and electromagnetic) full 3D CORC® model has been implemented
Current sharing between tapes and layers is guaranteed through a proper boundary condition
Model validated with respect experimental data
Improve the computational time and stabilization of the model
Evaluate the thermal stability of a CORC®
Apply the model to more than 3 layers
3D model of a bended CORC®

## Slide 29
Thank you for your attention!
See you in Honolulu!

## Slide 30: References
Status of CORC® cables and wires for use in highfield magnets and power systems a decade after their introduction, D.C. Van der Laan et al, 2019
Two-Dimensional Anisotropic Model of YBCO Coated Conductors, Casali et. al, 2015
In-Field Electrical Resistance at 4.2 K of REBCO Splices, J. Fleiter and A. Ballarino, et. al, 2017
Self-Consistent Modeling of the Ic of HTS Devices: How Accurate do Models Really Need to Be?, Grilli et. al, 2014
Performance correlation between YBa2Cu3O7-δ coils and short samples for coil technology development, X. Wang et. al, 2016
Study of magnetization loss of CORC cables using 3D T-A formulation, Y. Wang, 2019
3D quench modeling base on T-A formulation for high temperature superconductor CORC cables, Y. Wang, 2019
Developing a Vacuum Pressure Impregnation Procedure for CORC® Wires, J. Sterne et. al, MT27, 2021
Distributed fiber optic sensing to identify locations of resistive transitions in REBCO conductors and magnets, L. Luo et. al, MT27 2021
Calculations of the AC losses in superconducting cables and coils: Neumann boundary conditions of T-A formulation, S. Wang, 2022
Finite-Element Analysis of the Strain Distribution Due to Bending in a REBCO Coated Conductor for Canted Cosine Theta Dipole Magnet Applications , Pierro F. et al, 2019
Isotropic round-wire multifilament cuprate superconductor for generation of magnetic fields above 30 T, Larbalestier D.C., et. al, 2014