## Slide 1: MQXFA Test Results Overview & MQXFA07/08 Analysis
G. Ambrosio, P. Ferracin, G. Vallone and the MQXFA team
MDP meeting Feb. 1, 2023

## Slide 2: Acknowledgement
US HL-LHC Accelerator Upgrade Project (AUP)
  BNL: K. Amm, M. Anerella, A. Ben Yahia, H. Hocker, P. Joshi, J. Muratore, J. Schmalzle, H. Song, P. Wanderer
  FNAL: G. Ambrosio, G. Apollinari, M. Baldini, J. Blowers, R. Bossert, R. Carcagno, G. Chlachidze, J. DiMarco, S. Feher, S. Krave, V. Lombardo, C. Narug, A. Nobrega, V. Marinozzi, C. Orozco, T. Page M. Parker, S. Stoynev, T. Strauss, M. Turenne, D. Turrioni, A. Vouris, M. Yu
  LBNL: D. Cheng, P. Ferracin, L. Garcia Fajardo, E. Lee, M. Marchevsky, M. Naus, H. Pan, I. Pong, S. Prestemon, K. Ray, G. Sabbi, G. Vallone, X. Wang
  NHMFL: L. Cooley, J. Levitan, J. Lu, R. Walsh
CERN: HL-LHC Project
  G. Arnau Izquierdo, A. Ballarino, M. Bajko, C. Barth, N. Bourcey, B. Bulat, M. Cruovizier, A. Devred, H. Felice, S. Ferradas Troitino, L. Fiscarelli, J. Fleiter, M. Guinchard, O. Housiaux, S. Izquierdo Bermudez, N. Lusa, F. Mangiarotti, A. Milanese, A. Moros, P. Moyret, C. Petrone, J.C. Perez, H. Prin, R. Principe, E. Ravaioli, T. Sahner, S. Sgobba, P. Tavares Coutinho Borges De Sousa, E. Todesco, J. Ferradas Troitino, R. Van Weelderen, G. Willering

## Slide 3: Outline
MQXFA magnets
Fabrication and test status
Analysis of magnets with limited performance
  MQXFA07 and MQXFA08
Lessons learned and corrective actions
MQXFA endurance and resilience
Conclusions

## Slide 4: 20 MQXFA Magnets for HL-LHC Inner Triplets
10 Q1/Q3 Cryo-assemblies (including 2 spares)
2 magnets in each cryo-assembly

## Slide 5: MQXFA/B Design
Parameter | Unit | MQXFA/B
Coil aperture | mm | 150
Magnetic length | m | 4.2/7.15
N. of layers |  | 2
N. of turns Inner-Outer layer |  | 22-28
Operation temperature | K | 1.9
Nominal gradient | T/m | 132.2
Nominal current | kA | 16.23
Peak field at nom. current | T | 11.3
Stored energy at nom. curr. | MJ/m | 1.15
Diff. inductance | mH/m | 8.26
Strand diameter | mm | 0.85
Strand number |  | 40
Cable width | mm | 18.15
Cable mid thickness | mm | 1.525
Keystone angle |  | 0.4
P. Ferracin et al., “Development of MQXF, the Nb3Sn Low-β Quadrupole for the HiLumi LHC ” IEEE Trans App. Supercond. Vol. 26, no. 4, 4000207
Nb3Sn Conductor
RRP 108/127
G. Ambrosio et al., “First Test Results of the 150 mm Aperture IR Quadrupole Models for the High Luminosity LHC” NAPAC16, FERMILAB-CONF-16-440-TD
E. Takala et al., “Mechanical Comparison of Short Models of Nb3 Sn
Low-β Quadrupole for the Hi-Lumi LHC” IEEE TAS. Vol. 31, no. 5, 4000306

## Slide 6: MQXFA Fabrication Status
9 magnets have been assembled: MQXFA03-11
1 magnet has been disassembled after preload
  MQXFA09
8 magnets have been tested
  MQXFA03-08 and MQXFA10-11
1 magnet has been dis-assembled after test & re-assembled with a new coil
  MQXFA08  MQXFA08b
MQXFA03 during final preparation at LBNL
K. Ray et al., “Applied metrology for the assembly of Nb3Sn MQXFA quadrupole magnets for the HL-LHC AUP” 3LPo1A-02

## Slide 7: MQXFA Vertical Test
  MQXFA magnets are vertically tested at BNL
  Test plan demonstrates:
    Holding at Acceptance Current: Nominal + 300 A
    Temperature margin: Nominal curr. at 4.5 K
    Memory after thermal cycle
    Other requirements (next slide)
7
MQXFA @ BNL

## Slide 8: Vertical Test Summary
Magnets are accepted for use in LMQXFA Cold Mass if they meet all Vertical Test Requirements
  Hold current at nominal current + 300 A
  Field Quality
  Integrated gradient
  Ramp to/from I_nom at ±30 A/s
  100 A/s ramp down w/o quench (max for power supply)
  Temperature margin
  Training memory
  Splice resistance (less than 1 nW)
  All electrical requirements
S. Feher et al., “AUP first pre-series Cryo-Assembly Design Production and Test Overview” 2LOr2A-04

## Slide 9: Vertical Test: Training
MQXFA03-06 and MQXFA10-11 reached and held Acceptance Current and met all requirements tested at BNL
6 out of 8 magnets tested

## Slide 10: Integrated Gradient & Field Quality @ BNL
Mechanical data and analysis:
L. Garcia Fajardo et al., “Analysis of the mechanical performance of the 4.5 m long MQXFA Pre-Series magnets for the Hi-Lumi LHC Upgrade” 3LPo1A-01
Average IG at 16.23 kA: 561.92 T
In order to obtain a consistent comparison, correction factors were applied to several magnets to account for measurements taken at different currents as well as changes in the measurement setup and coil design
Courtesy of G. Sabbi and A. Ben Yahia
Field Quality in Straight Section vs expectation
Before b6 correction in cross-section

## Slide 11: Outline
MQXFA magnets
Fabrication and test status
Analysis of magnets with limited performance
  MQXFA07 and MQXFA08
Lessons learned and corrective actions
MQXFA endurance & resilience
Conclusions
US-HiLumi-doc-4293
CERN EDMS #2777612
https://inspirehep.net/literature?q=FERMILAB-TM-2789-TD

## Slide 12
Courtesy of J. Muratore and A. Ben Yahia
Location based on Quench Antenna and Voltage Taps
Reverse temperature dependence
Reverse ramp-rate dependence
Same features and location in MQXFA08

## Slide 13: Limitation “Mechanism”
Instability triggered by a local issue, likely affecting only some strands, that pushes more current in adjacent strand(s)
  Field in quenching turn is between 6 and 9 T
Similar mechanism in other magnets:
  MQXFS03 showed a reversible component
  LARP Long Quadrupole #2 showed “enhanced thermo-magnetic instability” in mid-plane block
  With flux jumps
H. Bajas et al., “Test Results of the Short Models MQXFS3 and MQXFS5 for the HL-LHC Upgrade”, IEEE Trans. Appl. Superc. Vol 28, # 4007006 (2018)
Ref: G. Ambrosio et al., “Progress in the Long Nb3Sn Quadrupole R&D by LARP”, IEEE Trans Appl, Superc. Vol 22, # 4003804 (2012)
B. Bordini, et al., IEEE Trans. Appl. Superc., vol. 22, 2012, # 4705804
A. K. Ghosh, IEEE Trans. Appl. Superc., vol. 23, 2013, # 7100407
…

## Slide 14: Coil Fabrication Analysis
A few discrepancies during fabrication:
  Some strands popped out during winding, were fixed, popped out overnight and were fixed a second time (BNL DR AM-164)
  Limiting coil was affected by COVID lockdown
    14 weeks stop after winding & curing of inner layer
  No other NCR nor traveler data anomaly
coil 214 as it was setup for the lab shutdown
Inner layer coil showing in yellow the position of coil-214 cable affected by DR AM-164
Courtesy of J. Schmalzle

## Slide 15: Structure Analysis & MQXFA07 Disassembly
Yoke
Al shell
Gap key
Cooling
holes
Collar
Pad
Pole key
Axial rod
location
Master
keys
Load
key
Bladder
location
A pole-key gap asymmetry was found during MQXFA07 and MQXFA08 disassembly:
- Gaps closed in quadrant 3
- Gaps open in other quadrants
Courtesy of P. Ferracin and D. Cheng
Q1
Q2
Q3
Q4

## Slide 16: Pole-key gaps in MQXFA07
The measured pole-key gaps were not as uniform in MQXFA07 and MQXFA08 as in past magnets; this is particularly apparent on the limiting coils (Q3 for both magnets)
Only the total average (on the 4 keys) was targeted in the specification. The underlying assumption was that the gaps would be redistributed across coils during loading.
Investigation of the effect of this non-uniformity on the mechanical performances with 2D and 3D FE models
  See next slides by P. Ferracin and G. Vallone
Courtesy of P. Ferracin and D. Cheng
LL1

## Slide 17: Finite element analysis Effect of a close pole key gap
Three different finite element models:
  360-degrees, full cross-section 2D model
  360-degrees, full cross-section 3D model (MQXFS)
  45-degrees, octant 3D model (MQXFS)
G. Ambrosio - MQXFA magnets - MDP mtg 2/1/23

## Slide 18: Finite element analysis 360-degrees, full cross-section 2D model
With a close pole key gap in Q3, the azimuthal pre-stress is:
  Significantly lower (~30 MPa reduction) in the Q3
  ‘Medium’ on the opposite side (Q1)
  “Maximum” on the two remaining quadrants
  No ‘dangerous’ stress/strain increase on the coil
This effect is not measured by the strain gauges
  However, measurement on a single axial location in RE
No ‘dangerous’ stress/strain on the coils
  MQXFS1 (short model) went over Iult with 85 MPa preload at cold
Q3
Q1
Q2
Q4
G. Ambrosio - MQXFA magnets - MDP mtg 2/1/23

## Slide 19: Finite element analysis 360-degrees, full cross-section 3D model
Axial behavior:
  No difference in the rods stress, but less force axial pre-load on the Q3 coil
    Lower azimuthal pre-stress results in less friction coil-structure  “axially softer coil”
G. Ambrosio - MQXFA magnets - MDP mtg 2/1/23

## Slide 20: Finite element analysis 360-degrees, full cross-section 3D model
“a3a4 LE area”
  Contact between wedge and end spacer in L1
  Considering bonded conditions
    Tension occurs in Q3 during excitation
  Debonding models show interfacial failure
G. Ambrosio - MQXFA magnets - MDP mtg 2/1/23

## Slide 21: Finite element analysis 45-degrees, octant 3D model
More detailed analysis using the octant model
  Not bonded, as if epoxy cracking has already occurred
  The gap between wedge and end-spacer induces a spike in axial strain in the coil which can reach the 0.4% level
    Larger increase in the pole block turn
G. Ambrosio - MQXFA magnets - MDP mtg 2/1/23
LL2

## Slide 22: Magnet Dis-assembly
Pressure imprint on the Kapton in Q3 pole-key gaps
  Absent in the other coils

## Slide 23
Unusual marks at wedge-spacer interface in the lead end of coil 214 (in Q3)

## Slide 24: Micrographic Analysis of Coil 214 Lead End
No anomalies found in cross-section #1.
Therefore, we did longitudinal sections
Analysis started with sample #1: wedge-spacer interface
CT-scan, dye-penetrant test and metallurgical analysis by CERN teams
Outstanding collaboration!
By M. Crouvizier, A. Moros, S. Sgobba, CERN
By B. Bulat, CERN
S. Sgobba et al., “Advanced Examination of Nb3Sn Coils and Conductors for the LHC luminosity upgrade: Computed Tomography and Materialographic Analyses”, this session

## Slide 25: Metallurgical inspection: the smoking gun!
Longitudinal cuts on cables adjacent to the end-spacer/copper-wedge transition
  Localized field of broken filaments (red dots), especially at pole block
By M. Crouvizier, A. Moros, S. Sgobba, CERN
# | Samples adjacent to W-S transition from coil 214 Lead End | Number of cracked filaments
1 | Layer-jump side, cable in midplane block, side adjacent to W-S transition | 0
2 | Layer-jump side, cable in pole block, side adjacent to W-S transition | 532
3 | Non-layer-jump side, cable in midplane block, side adjacent to W-S transition | 54
4 | Non-layer-jump side, cable in pole block, side adjacent to W-S transition | 728
5 | Same cable of sample 4, side opposite to the W-S transition | 0

## Slide 26: MQXFA08 Analysis
Same features as in MQXFA07
Metallographic analysis of lead end shows broken filaments at wedge-spacer interface
By M. Crouvizier, A. Moros, S. Sgobba, CERN
S. Sgobba et al., “Advanced Examination of Nb3Sn Coils and Conductors for the LHC luminosity upgrade: Computed Tomography and Materialographic Analyses”, this session

## Slide 27
Based on these findings, we understand that coil 214 pole-key gaps were closed at cold, whereas those of other coils were open. During magnet energization this difference caused tensile strain at wedge-spacer interfaces in coil 214 ends. In early ramps to quench (possibly before or during ramp #4) the bonding between the copper wedge and the resin (filled with S-e glass) gave away in the lead end increasing the strain on the strands closest to that interface. The “increased” strain degraded some strands and triggered the enhanced self-field instability behavior. This mechanism caused quench #4 and all subsequent quenches at 1.9 K and 20 A/s.
These quenches with hot-spot close to the wedge-spacer interface may have exacerbated this mechanism increasing the local strain and strand damage, and therefore causing the current drop (~1 kA) from quench #4 to #8.

## Slide 28: Covid impact
Changes to assembly procedures caused by COVID requirements
  #1: change in bolting procedure for increasing tech distance
  #2: the technician who had been leading the coil-pack assembly operations was removed from that task (starting from MQXFA06) because not vaccinated.
COVID lockdown
   Stop in fabrication of coil 214 after Inner-Layer was cured may have weakened wedge-spacer bond
Less supervision caused by COVID
   increased probability of non-uniform pole-key gaps and other differences.
Courtesy of P. Ferracin and D. Cheng

## Slide 29: Preventive Actions
In order to prevent reoccurrence of this issue,
Design change for larger pole-key gaps:
  From 200 mm to 400 mm - average pole key gap per side
Revised MQXFA Series Magnet Production Specification:
  Added spec for minimum gap on each coil at each longitudinal location: 300 mm per side
MQXFA10 Quench History
MQXFA10 Pole-key gaps
Courtesy of A. Ben Yahia
Courtesy of P. Ferracin
D. Cheng et al., “The challenges and solutions of meeting the assembly specifications for the 4.5 m long MQXFA magnets for the Hi-Luminosity LHC” 2LOr2A-02

## Slide 30: Endurance Tests
Previous endurance tests were successfully performed on short models
MQXFA05 met requirements after 5 thermal cycles, 52 quenches and 79 powering cycles
5 Thermal cycles
52 quenches (10 spontaneous + 42 induced)
79 power cycles (52 quenches + 27 cycles w/o quench) above 10 kA.

## Slide 31: MQXFA11 “Resilience Test”
The truck transporting the MQXFA11 magnet from LBNL to BNL was rear ended by another truck.
The main hit took place on the right back corner. During the incident the truck rear axle disengaged as displayed below. Nobody was injured.
The magnet was moved to FNAL. Upon arrival a visual inspection was performed followed by electrical checkout, metrology survey, analysis of the fiber optic sensors and accelerometer data analysis
  Max shock: 6 or 10 g vertical (depending on the device in the same accelerometer unit)
  Duration: 5 ms
All tests and analyses were OK. Magnet was shipped to BNL
Courtesy of J. Blowers
Courtesy of T. Cruise

## Slide 32: MQXFA11 “Maverick” Quench History
Courtesy of A. Ben Yahia

## Slide 33: Conclusions
6 out of 8 successful MQXFA vertical tests
MQXFA07/08 “smoking gun” was found
  Mechanism is understood
  Covid restrictions and lockdown contributed to the degradation mechanism
  Design change (larger gaps) and Specification revision (minimum gaps spec.) are going to prevent reoccurrence in future magnets
  MQXFA10 & MQXFA11 demonstrated that this issue is over
MQXFA05 demonstrated Endurance
MQXFA11 demonstrated Resilience

## Slide 34: Backup Slides

## Slide 35: MQXFA08 Quench History
Fixed 42-nohm splice to test facility
Connected voltage taps to coil 213 LE

## Slide 36: Assessment of MQXFA Data & Travelers
Completed assessment of travelers for Coil Fabrication at BNL, and Magnet Assembly at LBNL:
Assessment of coil parameters, which are being tracked, did not show any anomaly
Coil traveler assessment did not show any issue in addition to known DRs
Assessment of magnet assembly & preload data in next slides

## Slide 37
Left: coil section after samples were extracted for metallographic inspection.
Center: color scheme used to show the position of filament cracks with respect to the W-S transition in the following figure. A: End spacer + ceramic coating ≈ 0,5 mm; B: resin (filled with S-2 glass) between end spacer and wedge ≈ 1,5 mm; C: copper wedge.
Right: color scheme applied on sample with broken filaments.
Copper wedge
End spacer & ceramic coating
Resin with S-2 glass
By M. Crouvizier, A. Moros, S. Sgobba, CERN