## Slide 1
Vittorio Marinozzi
03-21-2023
Quench protection of a 20 T hybrid dipole magnet

## Slide 2: Analyzed magnet
  20 T cos-theta
  6 layers (2 Bi2212 + 4 Nb3Sn)
  Current: 13.5 kA
  Inductance: 63 mH/m
  Stored Energy: 4.4 MJ/m
  Other hybrid magnets have similar parameters
    Common-coil is double aperture
Margin and mechanics are ok
V. Marinozzi, et al., Conceptual Design of a 20 T Hybrid Cos-Theta Dipole Superconducting Magnet for Future High-Energy Particle Accelerators, IEEE Trans. on Appl. Supercond., 2023
Bi2212
Nb3Sn
Nb3Sn

## Slide 3: Why is protection challenging
  High magnetic field, large stored energy
  Slow detection in HTS
  Large current density in copper (~1.3 kA/mm2)
  Many layers and interfaces (peak voltages)

## Slide 4: Conductor parameters and MIITs
Parameter | Layer 1-2 | Layer 3-4 | Layer 5-6
Material | Bi2212 | Nb3Sn | Nb3Sn
Stabilizer | Ag | Cu | Cu
RRR | 100 | 100 | 100
Stabilizer/Superconductor | 3 | 1 | 1.45

## Slide 5: Assumptions for quench simulation
  Simulations made with STEAM-LEDET
  Simulations made for a short magnet (1 m)
  Hot spot temperature computed with adiabatic assumptions
  Fixed quench detection time: 15 ms
  Dump resistor of 74 mΩ, dimensioned to have 1 kV between magnet leads (500 V to ground with symmetric grounding)
  CLIQ unit based on existing CLIQ unit used for AUP magnets
    1 kV
    40 mF
  No quench heaters

## Slide 6: Protection of a 1 m magnet with dump resistor
Peak temperature is 640 K in LTS, 280 K in HTS

## Slide 7: Protection of a 1 m magnet with CLIQ
Peak temperature is 550 K in LTS, 250 K in HTS

## Slide 8: Why high temperature in LTS
4 inner layers are cold due to low resistivity respect to layers 5-6

## Slide 9: Optimizing CLIQ
Cliq can be optimized by improving current change directions
40 K less, still too high temperature

## Slide 10: Optimizing CLIQ with dump resistor
74 mΩ dump resistor can improve CLIQ efficiency furthermore (~80 % of the magnet quenched instantaneously), resulting in 400 K in LTS (~100 K reduction)

## Slide 11: Temperature distribution with CLIQ + dump
Still, innermost layers are cold with respect to layers 5-6
  The difficulty is not quenching the magnet, but heating it up to develop resistance
Layers 5-6
Layers 1-4

## Slide 12: Peak voltages to ground and turn-turn
Dump
Turn-turn
To-Ground
CLIQ
CLIQ optimized
CLIQ + dump

## Slide 13: Quench Protection resume
Parameter | Dump | CLIQ | Optimized CLIQ | CLIQ + Dump
HTS Hot Spot temerature [K] | 280 | 250 | 230 | 190
LTS Hot Spot temerature [K] | 640 | 550 | 510 | 400
Peak voltage to ground [V] | 500 | 500 | 800 | 1500
Peak turn-turn voltage [V] | 23 | 21 | 23 | 37

## Slide 14: Possible solutions for improvement
The main problem is that the four innermost layers don’t heat up due to low resistivity
Solution 1: reduce RRR (or reduce amount of stabilizer) in layers 1-4
  Cons: instabilities, cable production
Solution 2: increase dimension of layer 5-6 conductor
  Cons: cost increase, size increase, maybe mechanics
  Also, RRR of layer 5-6 conductor can be increased to reduce resistivity
Solution 3: reduce conductor size in layer 1-4
  Cons: not much margin to play with, mechanics, inductance increase if adding turns
Separate HTS and LTS circuits
  Out of Working Group assumptions (series powering)
  Voltages?

## Slide 15: Conclusions and next steps
The quench protection of the 20 T hybrid cos-theta looks very challenging
  Difficult to keep the hot spot temperature within 350 K for the LTS
  The most optimal is 400 K
  Still work in progress, lot of margin for improvement!
The HTS is protectable (< 300 K) (but detection technique is to be defined)
Peak voltage reaches 1.5 kV in the most efficient scenario, turn-turn voltage is ok
  A long magnet will likely have larger peak voltages
Next steps
  Optimization of the magnetic design to improve quench protection
    Increase of layer 5-6 conductor size looks the more promising
  Parametric study of the temperature with respect of conductor RRR
  Further CLIQ optimization (not HiLumi based)
  Quench heaters addition
  Evaluation of detection techniques and detection time for the HTS
  Protection of other hybrid magnets (Block-Coils, Common-Coils)