## Slide 1: The short model program of Nb3Sn quadrupoles for the HiLumi LHC and its potential
Paolo Ferracin, Giorgio Ambrosio, Susana Izquierdo Bermudez, Ezio Todesco
on behalf of the MQXF collaboration
International Particle Accelerator Conference (IPAC)
Venice, Italy
May 7-12, 2023

## Slide 2: Acknowledgements
US HL-LHC Accelerator Upgrade Project (AUP)
  BNL: K. Amm, M. Anerella, A. Ben Yahia, H. Hocker, P. Joshi, J. Muratore, J. Schmalzle, H. Song, P. Wanderer
  FNAL: G. Ambrosio, G. Apollinari, M. Baldini, J. Blowers, R. Bossert, R. Carcagno, G. Chlachidze, J. DiMarco, S. Feher, S. Krave, V. Lombardo, C. Narug, A. Nobrega, V. Marinozzi, C. Orozco, T. Page M. Parker, S. Stoynev, T. Strauss, M. Turenne, D. Turrioni, A. Vouris, M. Yu
  LBNL: D. Cheng, P. Ferracin, L. Garcia Fajardo, E. Lee, M. Marchevsky, M. Naus, H. Pan, I. Pong, S. Prestemon, K. Ray, G. Sabbi, G. Vallone, X. Wang
  NHMFL: L. Cooley, J. Levitan, J. Lu, R. Walsh
CERN
  S. Izquierdo Bermudez, E. Gautheron, G. Kirby, A. Foussat, J. Carlos Perez, F. Rodriguez Mateos, N- Lusa, E. Ravaioli, M. Bednarek, J. Ferradas Troitino, F. Mangiarotti, M. Bajko, A. Devred, H. Felice, D. Perini, G. Willering, S. Ferradas Troitino, H. Prin, A. Milanese, J. Ferradas Troitino, E. Takala, R. Principe, A. Ballarino, D. Tommasini, B. Bordini, J. Fleiter, C. Barth, S. Hopkins, F. Savary, D. Duarte Ramos, Y. Leclercq, M. Struik, L. Fiscarelli, S. Russenschuck, C. Petrone, G. de Rijk, L. Rossi, P. Fessia, S. Riebe, H. Garcia Gavela, L. Carlos, S. Fleury, G. Vandoni, L. Quain Solis, A. Dallocchio, P. Moyret, S. Sgobba, A. Moros, M. Crouvizier, B. Bulat, M. Guinchard and its team, et al.

## Slide 3: Outline
Introduction and program goals
Magnet design
Program overview
Performance overview
Additional studies and outcomes
Conclusions

## Slide 4: Introduction From LHC to HL-LHC
HL-LHC goals
  Extend LHC life time by 15+ years
  Prepare the machine for producing in that period 10 times more data as compared to the nominal LHC operation period
Overall status of the HL-LHC project (TUYG1) by O. Bruning

## Slide 5: Introduction HL-LHC Interaction Region
New inner triplet quadrupole
  Larger aperture to reduce the beam size: from 70 to 150 mm
  Nb-Ti to Nb3Sn  only 8 m longer than in the LHC (23 m  31 m)
LHC
HiLumi LHC
132.2

## Slide 6: Introduction from LHC to HL-LHC low- quadrupoles
Everything significantly increased
  strand…cable…coil…structure
From 70 mm to 150 mm aperture
From Nb-Ti at 8.6 T to Nb3Sn at 11.3 T
~4 times the e.m. forces in straight section
LHC low- quadrupoles
HL-LHC low- quadrupoles

## Slide 7: Introduction LHC dipole vs HL-LHC low- quadrupole
  Nb-Ti
  8.3 T
  _e.m.= 50-60 MPa
  Nb3Sn
  11.3 T
  _e.m.= 100-110 MPa

## Slide 8: Introduction HiLumi low-β quadrupole MQXF
Nominal conditions (7 TeV operation)
  Gnom=132.2 T/m
  11.3 T Bpeak_nom
  ~77% of Iss
Ultimate conditions (7.5 TeV operation)
  Gult=142.1 T/m
  12.1 T Bpeak_ult
  ~83% of Iss
Iult

## Slide 9: Introduction HiLumi low-β quadrupole MQXF
Different lengths, same design, very similar assembly procedure and loading target
MQXFS
(1.2 m)
MQXFA
(4.2 m)
MQXFB
(7.2 m)
A. Milanese, WEPM060
MQXFS
AUP MQXFA
CERN MQXFB
G.Apollinari, MOPL040
Joint CERN-LARP short model development program (MQXFS) to validate the design

## Slide 10: Outline
Introduction and program goals
Magnet design
Program overview
Performance overview
Additional studies and outcomes
Conclusions

## Slide 11: Magnet design
150 mm aperture
Double layer coil wound with 18 mm wide cable
Support structure based on aluminum shell pre-loaded with bladders and keys
Axial support with end-plate and axial rods
Al/SS

## Slide 12: Outline
Introduction and program goals
Magnet design
Program overview
Performance overview
Additional studies and outcomes
Conclusions

## Slide 13: Program overview
7 magnets
  2 LARP/AUP-CERN
  5 CERN
27 coils tested
  4 conductors
46 tests
  7 “virgin”
  20 modifications
  19 thermal cycles

## Slide 14: Program overview Timeline
7 models built, 6 conform
14
T0: aperture and cable selection
2013
2014
2015
2016
2017
2018
2019
2020
2021
MQXFS1: ≥ 12.9 T
MQXFS3: ≥ 11.8 T
MQXFS5: ≥ 12.7 T
MQXFS4: ≥13.1 T
MQXFS6: ≥13.3 T
MQXFS7: ≥13.2 T
RED indicates conform magnets
2022
MQXFS8: ≥12.0 T
2023
11.3 T Bpeak_nom
12.1 T Bpeak_ult

## Slide 15: Outline
Introduction and program goals
Magnet design
Program overview
Performance overview
Additional studies and outcomes
Conclusions

## Slide 16: The early magnets MQXFS1: the first one
Designed and fabricated by multiple laboratories
CERN
FNAL
BNL
LBNL
Coils 103-104
Structure 1
Coil 3-5
Coil 3-5
MQXFS1

## Slide 17: The early magnets MQXFS1: the first one
1a: ultimate passed, relatively long training, perfect memory
  Validation of coil fabrication and mechanical design
Then 1b, explore different pre-load conditions
  Still ok, but more erratic

## Slide 18: The early magnets MQXFS3: the second one
S3a: still higher azimuthal pre-load
  Good start, but then de-training
S3b: higher axial pre-load
  Improvement but still limited at 1.9 K
Visual inspection: broken pole key

## Slide 19: The early magnets MQXFS4
Pre-load
  We targeted “nominal” for azimuthal and axial and pole key gap
Excellent training and memory 
  Set as reference for sub-sequent short and long magnets

## Slide 20: Performance overview Maximum field (T)
All the magnets passed nominal
All but S3 passed ultimate (S8 training not completed)
The 13 T level reached, with the exception of S3
  1.5 T more than needed at nominal

## Slide 21: Relevance to current magnet programs
MQXF
13T
CERN HFM & US MDP
Nb3Sn program (12-14T)
By L. Bottura
US MDP
HTS/Nb3Sn program (~20T)

## Slide 22: Performance overview Maximum current (Iss %)
The 90-95% level reached at 1.9 K and 4.5 K
  S3 at 1.9 K limited at 80% at 1.9 K
  S8 training not completed
1.9 K
4.5 K

## Slide 23: Outline
Introduction and program goals
Magnet design
Program overview
The early magnets
Performance overview
Additional studies and outcomes
Conclusions

## Slide 24: Endurance
Long-term behavior investigated in MQXFS4
No degradation after 11 thermal cycles (a to e) and 1000 current cycles (c)
  Endurance tested successfully on other short models and long magnet
No re-training after thermal cycle

## Slide 25: Superconductor validation
4 Bruker-OST strands used during the short
  RRP 108-127 chosen for the project
    Sufficiently small filament and lower cost
  In addition
    RRP 132/169, PIT 192, and PIT 192 with bundle barrier
Ultimate passed with all strands (also mixed)
RRP 108/127
PIT 192
RRP 132/169
PIT 192 bundle

## Slide 26: Training/plateau vs. pre-stress (I)
Impact of pre-stress on training/plateau investigated with MQXFS6
Wide pre-load window to reach ultimate current (-75 to -120 MPa)
Indication that larger preload is beneficial to reach higher plateau 90% of Iss

## Slide 27: Training/plateau vs. pre-stress (II)
Impact of pre-stress on training/plateau further investigated with MQXFS7
Wider pre-load window to reach ultimate current (-75 to -170 MPa)
  …to be continued

## Slide 28: Quench protection
Stored energy density in the coil is 50% higher than for LHC dipoles
Two systems
  Outer layer quench heaters
  Coupling-Loss Induced Quench (CLIQ) System
Both performing as expected
  Tpeak < 350 K with QH only and < 250 K with both
In MQXFS4 no sign of degradation to Iult high QI test reaching a Thot ≈ 400 K

## Slide 29: Field quality
Field quality either in spec or correctable with shims
Lesson learned from short models
  Magnetic shimming validated
  Correction of b6 with pole and mid-plane shims
  The dominant source of errors is coil geometry and its initial assembly in the coil pack (before pre-loading)
See A. Milanese, WEPM060

## Slide 30: Outline
Introduction and program goals
Magnet design
Program overview
The early magnets
Performance overview
Additional studies and outcomes
Conclusions

## Slide 31: Conclusions
MQXF short models: collaborative effort of 4 different labs
7 magnets fabricated and tested
6 out of 7 reached ultimate
Maximum field level of 13 T
  Relevant for both CERN HFM and US MDP magnet program
90-95% of Iss both at 1.9 K and 4.5 K
No degradation after thermal cycles and current cycles
No re-training after thermal cycle
A wide pre-load window to reach ultimate demonstrated
  From -75 MPa to -170 MPa after cool down
Validation of QP, insulation and correction of magnetic errors

## Slide 32
Thank you