## Slide 1: MDP Technical Meeting #5 on 20 T hybrid magnet and comparative analysis
P. Ferracin, G. Ambrosio, E. Barzi, L. Cooley, R. Gupta, V. Kashikhin, V. Marinozzi, I. Novitski, A. Zlobin
US Magnet Development Program

## Slide 2: Outline
Definition of the goals of the working group
Design criteria for a 20 T hybrid magnet
Some preliminary estimates of radiuses and dimensions
Overview of current hybrid work
Action items

## Slide 3: 1st goal of the working group
Conceptual design of a 20 T hybrid HTS-LTS magnet
  Comparative analysis of different design options for a 20 T hybrid
    Cos design and its stress-management options
      “Traditional” Cos
      Canted Cos (CCT)
      Stress management Cos (SMCT)
    Block-type coil design (block with flared ends)
    Common-coil design (block with racetrack coil)
  Definition of general design criteria: aperture, field, margin…..
  Analysis of challenges specifically of hybrid magnets
    Integration of LTS/HTS, mechanics, protection, powering, diagnostics, test facility…..

## Slide 4: 1st goal of the working group
An example: 16 T dipole magnets for FCC
Ideally the goal should be to carried out the full 2D design and analysis of a 20 T hybrid for all the design options considered
    Cos design and its stress-management options, Block-type design, Common-coil design
In addition, 3D considerations will be included in the comparison

## Slide 5: 1st goal of the working group
The goal of the comparison should not be, or does not necessarily have to be
  reaching a consensus on a particular design
Instead, more realistically, the working group could aim at
  Discussing and reviewing the different designs and listing pluses and minuses or open issues….grounding on “objective” criteria
  Providing inputs to the other areas (in particular area I and area II) to better define their roadmaps and overall directions, and avoid inconsistencies

## Slide 6: 1st goal of the working group
Time frame: 2020 – 2023
Methods
  Modeling effort
    “classical 2D/3D” mechanical, magnetic and QH simulations
      Developing new modeling techniques is not part of this task
      However, if new tool/analysis is required  feed-back to Technology area (III), modeling and simulations

## Slide 7: 2nd goal of the working group
Review and follow-up of current work towards 9-15 T hybrid magnets
  This current work can be divided based on the field level
    9-10 T
    11-12 T
    13-14 T
    Beyond 15 T
  The goal is to collect and organize information from these programs (responsibility of area I and area II) to provide inputs for 20 T hybrid design

## Slide 8: Outline
Definition of the goals of the working group
Design criteria for a 20 T hybrid magnet
Some preliminary estimates of radiuses and dimensions
Overview of current hybrid work
Action items

## Slide 9: Design criteria for a 20 T hybrid magnet
Previous work within MDP on a 16 T dipole magnet
  GianLuca Sabbi, Alexander Zlobin, MDP General meeting – May 17, 2017
https://conferences.lbl.gov/event/82/

## Slide 10: Design criteria for a 20 T hybrid magnet
Geometrical
  Number of apertures 1
  Free coil aperture 50 mm
Comments
  The common coils will naturally provide 2 apertures
    This will be taken into account on the comparison
  No “strong” constraints on
    Magnet total length (<2 m)
    Magnet straight section (>200 mm)
    Maximum magnet OD
      Reference numbers: 620 mm (FNAL/1.9K), 660 mm (BNL/1.9K), 914 mm (LBNL/4.5K)

## Slide 11: Design criteria for a 20 T hybrid magnet
Operational
  Reference temperature 1.9 K
    4.5 K option can be considered: it would impact the ratio of HTS vs LTS
  Operational bore field 20 T
  Margin on the load-line @ 1.9K 15 %
    With respect to round strand Ic including self field and 5% cabling degradation
  Short sample bore field 23.5 T
  Geometrical harmonics at Rref=17 mm and 20 T: bn<5 for n<10
    Magnet straight section
  Target design field 20 T

## Slide 12: Design criteria for a 20 T hybrid magnet
Operational
  Maximum Nb3Sn coil stress >180 (<150) MPa at 1.9 (293) K
  Conditions of coil-pole or rib interfaces at 20 T
    If bonded 20 MPa max. tension
      ‘Corner spikes’ (~1 contact element, 1 mm) neglected
    If separation allowed: Half cable width in contact or < 50 µm max gap
      Conditions may be different depending on the design

## Slide 13: Design criteria for a 20 T hybrid magnet
Bonded vs separation-allowed
  Test Facility Dipole (by G. Vallone)

## Slide 14: Design criteria for a 20 T hybrid magnet
Bonded vs separation-allowed
  MQXF (by G. Vallone)

## Slide 15: Material limits (by Giorgio Vallone)

## Slide 16: Design criteria for a 20 T hybrid magnet
Nb3Sn Conductor and cable
  Strand diameter 0.7-1.2 mm
  Cu:non-Cu ratio 0.8-2.0
  Non-Cu Jc round strand with self-field
    12 T, 4.2 K 2980 A/mm2
    15 T, 4.2 K 1640 A/mm2
    16 T, 4.2 K 1250 A/mm2
      See next slide for reference fit
      It may be difficult to achieve this in small diameter strands…..
  RRR (after cabling) >50
  Ic degradation due to cabling 5%
  Maximum number of strands in cable 60
  Cable Insulation thickness 0.150 mm

## Slide 17: Design criteria for a 20 T hybrid magnet
Nb3Sn Conductor and cable
Reference Jc(B,T) fit:
  , ,
  where 𝑡=𝑇/𝑇c0; 𝑏=𝐵p/𝐵c2 (𝑡), Bp is the conductor peak field, Tc0 = 16 K, Bc20 =29.77 T, C0 = 223900 T.A/mm2.
Fit of data from recent (03/2020) RRP 108/127, 1.1 mm diameter, 1.1 Cu/non-Cu

## Slide 18: Design criteria for a 20 T hybrid magnet
Nb3Sn Conductor and cable
  “3000” A/mm2 kind of conductor, round, with self field
Jc round
Jc , 5% deg.
Je , 5% deg.

## Slide 19: Design criteria for a 20 T hybrid magnet
Nb3Sn Conductor and cable
  In general, it would be better to stay within already tested parameters (min, max)
Dimension before reaction; In MQXF, assumed expansion during reaction is 4.5 % (th), 1.2 % (w)

## Slide 20: Design criteria for a 20 T hybrid magnet
Bi2212 Conductor and cable (input from T. Shen and L. Garcia Fajardo)
  The wire diameter:
    from 0.6 mm to 1.5 mm
  Cable width: basically same possibilities as with Nb3Sn cables

## Slide 21: Design criteria for a 20 T hybrid magnet
Bi2212 Conductor and cable (input from T. Shen and L. Garcia Fajardo)
  Record performance strand RC5/6 about 20% higher than what is currently “comfortably” produced.

## Slide 22: Design criteria for a 20 T hybrid magnet
REBCO Conductor and cable
  Maximum Nb3Sn coil stress: <120 MPa (293) K

## Slide 23: Design criteria for a 20 T hybrid magnet
Quench protection
  Maximum hot spot temperature 350 K
    Failure scenarios?
  Total time delay 40 ms
  Maximum voltage to ground @ quench 1.0 kV
  Ground insulation design voltage >5 kV
  Powering in series or independent?
    I would propose in series
  What about a maximum J in the Cu of 1500 A/mm2 ?
    It would provide a quick/easy check and limits of the grading options

## Slide 24: Outline
Definition of the goals of the working group
Design criteria for a 20 T hybrid magnet
Some very preliminary estimates of radiuses and dimensions
Overview of current hybrid work
Action items

## Slide 25: First some references (20 T Bop)

## Slide 26: First some references (“towards” 20 T)

## Slide 27: Nb3Sn aperture in a 20 T hybrid
With properties describe above Nb3Sn and Bi2212 cross at 14.5 T at 4.2 K and 16.5 T at 1.9 K

## Slide 28: Field in at 20 T dipole
Bbore_op = 20 T
Bpeak_op = Bbore_op · 1.04 = 20.8 T
Bbore_ss = Bbore_op / 0.85 = 23.5 T
Bpeak_ss = Bbore_ss · 1.04 = 24.4 T

## Slide 29: Analysis of interface diameter
Analytical model from Lucas Brouwer

## Slide 30: Analysis of interface diameter
Thick shell with cos distribution
  Bore field = conductor peak field
4 CCT winding layers,
  2 of Bi2212 and 2 of Nb3Sn
Field in Nb3Sn is given by self field + stray field from Bi2212 insert
From Je to Joverall keeping into account spar and ribs

## Slide 31: Analysis of interface diameter
Results: 150-160 mm interface diameter for a 23.5 T magnet

## Slide 32: Analysis of coil radius and thickness
Sector coil (60) with J = J0 distribution

## Slide 33: Analysis of coil radius and thickness

## Slide 34: Very…very…preliminary coil size
So, with Jo_op = 385 A/mm2 and Bbore_op = 20 T
  Coil width ~ 75 mm
Very strong assumptions
  constant uniform Jo,
    same cable….
  No spar/ribs…
75 mm should a first order thickness of only the “cable layers” in a cos distribution

## Slide 35: Field in the conductor
At short sample, Bp_ss = 24.4 T  Je_ss = 670 A/mm2  Jo_ss = 452 A/mm2
So, at 85% of short sample  Je_op = 570 A/mm2  Jo_op = 385 A/mm2

## Slide 36: Very…very…preliminary coil size
50 mm aperture
Under the previous assumption (very simple analytical model, no stress management….)
  ID Nb3Sn = 146 mm
  OD Nb3Sn = 200 mm
  75 m total coil thickness
    48 mm thick Bi2212 coil
    27 mm thick Nb3Sn coil

## Slide 37: Peak stress
Stress due to accumulated e.m. forces on the mid-plane
  No shear, no bending….

## Slide 38: Very…very…preliminary magnet size
20 mm collar
250 mm thick yoke
50 mm thick shell
  Fx/t = 200 MPa
OD: 850 mm

## Slide 39: Size comparison
LHC MQXF FRESCA2 ????

## Slide 40: Outline
Definition of the goals of the working group
Design criteria for a 20 T hybrid magnet
Some preliminary estimates of radiuses and dimensions
Overview of current hybrid work
  Both conceptual design and “real” development
Action items

## Slide 41: The 9-10 T field level
LBNL
  Bi2212 insert Bin5c_2 (2-3 T stand alone) in CCT5 (8-9 T)
    Test planned in 2021

## Slide 42: The 11-12 T field level
BNL
  Coils wound with REBCO tape or CORC (1-3 T) inside DCC017 common coil Nb3Sn dipole (10.2 T)
Tape perpendicular to field
Tape parallel to field
CORC

## Slide 43: The 13-14 T field level (I)
LBNL
  Bi2212 or REBCO (CCT or COMB) inserts (5-6 T stand alone) in CCT6 (2 or 4 layers, 11 T)

## Slide 44: The 13-14 T field level (II)
FNAL
  Bi2212 or REBCO (CCT or COMB) inserts (5-6 T stand alone) in SMCT (2 layers, ~11 T)

## Slide 45: The 13-14 T field level (III) and beyond 15 T
FNAL
  Bi2212 insert SMCT (4-5 T stand alone) in 11T dipole coil and then in SMCT coil

## Slide 46: Action items
Define “comparison” criteria
Define CORC specs and Je
Continue aperture/thickness/dimension analysis
  Iron, grading
  Move progressively from analytical model to simplified FEM of CT, CCT, SMCT, block and CC designs
Continue the update of current hybrid program